SECTION 01 45 29
TESTING LABORATORY SERVICES

PART 1 - GENERAL

1.1 DESCRIPTION:

This section specifies materials testing activities and inspection services required during project construction to be provided by a Testing Laboratory retained by the General Contractor.

1.2 APPLICABLE PUBLICATIONS:

A.	The publications listed below form a part of this specification to the extent referenced. The publications are referred to in the text by the basic designation only.

B.	American Association of State Highway and Transportation Officials (AASHTO):

T27-11	Standard Method of Test for Sieve Analysis of Fine and Coarse Aggregates

T96-02 (R2006)	Standard Method of Test for Resistance to Degradation of Small-Size Coarse Aggregate by Abrasion and Impact in the Los Angeles Machine

T99-10	Standard Method of Test for Moisture-Density Relations of Soils Using a 2.5 Kg (5.5 lb.) Rammer and a 305 mm (12 in.) Drop

T104-99 (R2007)	Standard Method of Test for Soundness of Aggregate by Use of Sodium Sulfate or Magnesium Sulfate

T180-10	Standard Method of Test for Moisture-Density Relations of Soils using a 4.54 kg (10 lb.) Rammer and a 457 mm (18 in.) Drop

T191-02(R2006)	Standard Method of Test for Density of Soil In-Place by the Sand-Cone Method

T310-13	Standard Method of Test for In-place Density and Moisture Content of Soil and Soil-aggregate by Nuclear Methods (Shallow Depth)

C.	American Concrete Institute (ACI):

506.4R-94 (R2004)	Guide for the Evaluation of Shotcrete

D.	American Society for Testing and Materials (ASTM):

A370-12	Standard Test Methods and Definitions for Mechanical Testing of Steel Products

A416/A416M-10	Standard Specification for Steel Strand, Uncoated Seven-Wire for Prestressed Concrete

C31/C31M-10	Standard Practice for Making and Curing Concrete Test Specimens in the Field

C33/C33M-11a	Standard Specification for Concrete Aggregates

C39/C39M-12	Standard Test Method for Compressive Strength of Cylindrical Concrete Specimens

C109/C109M-11b	Standard Test Method for Compressive Strength of Hydraulic Cement Mortars

C136-06	Standard Test Method for Sieve Analysis of Fine and Coarse Aggregates

C138/C138M-10b	Standard Test Method for Density (Unit Weight), Yield, and Air Content (Gravimetric) of Concrete

C140-12	Standard Test Methods for Sampling and Testing Concrete Masonry Units and Related Units

C143/C143M-10a	Standard Test Method for Slump of Hydraulic Cement Concrete

C172/C172M-10	Standard Practice for Sampling Freshly Mixed Concrete

C173/C173M-10b	Standard Test Method for Air Content of freshly Mixed Concrete by the Volumetric Method

C330/C330M-09	Standard Specification for Lightweight Aggregates for Structural Concrete

C567/C567M-11	Standard Test Method for Density Structural Lightweight Concrete

C780-11	Standard Test Method for Pre-construction and Construction Evaluation of Mortars for Plain and Reinforced Unit Masonry

C1019-11	Standard Test Method for Sampling and Testing Grout

C1064/C1064M-11	Standard Test Method for Temperature of Freshly Mixed Portland Cement Concrete

C1077-11c	Standard Practice for Agencies Testing Concrete and Concrete Aggregates for Use in Construction and Criteria for Testing Agency Evaluation

C1314-11a	Standard Test Method for Compressive Strength of Masonry Prisms

D422-63(2007)	Standard Test Method for Particle-Size Analysis of Soils

D698-07e1	Standard Test Methods for Laboratory Compaction Characteristics of Soil Using Standard Effort

D1140-00(2006)	Standard Test Methods for Amount of Material in Soils Finer than No. 200 Sieve

D1143/D1143M-07e1	Standard Test Methods for Deep Foundations Under Static Axial Compressive Load

D1188-07e1	Standard Test Method for Bulk Specific Gravity and Density of Compacted Bituminous Mixtures Using Coated Samples

D1556-07	Standard Test Method for Density and Unit Weight of Soil in Place by the Sand-Cone Method

D1557-09	Standard Test Methods for Laboratory Compaction Characteristics of Soil Using Modified Effort (56,000ft lbf/ft3 (2,700 KNm/m3))

D2166-06	Standard Test Method for Unconfined Compressive Strength of Cohesive Soil

D2167-08)	Standard Test Method for Density and Unit Weight of Soil in Place by the Rubber Balloon Method

D2216-10	Standard Test Methods for Laboratory Determination of Water (Moisture) Content of Soil and Rock by Mass

D2974-07a	Standard Test Methods for Moisture, Ash, and Organic Matter of Peat and Other Organic Soils

D3666-11	Standard Specification for Minimum Requirements for Agencies Testing and Inspecting Road and  Paving Materials

D3740-11	Standard Practice for Minimum Requirements for Agencies Engaged in Testing and/or Inspection  of Soil and Rock as used in Engineering Design and Construction

D6938-10	Standard Test Method for In-Place Density and Water Content of Soil and Soil-Aggregate by Nuclear Methods (Shallow Depth)

E94-04(2010)	Standard Guide for Radiographic Examination

E164-08	Standard Practice for Contact Ultrasonic Testing of Weldments

E329-11c	Standard Specification for Agencies Engaged in Construction Inspection, Testing, or Special Inspection

E543-09	Standard Specification for Agencies Performing Non-Destructive Testing

E605-93(R2011)	Standard Test Methods for Thickness and Density of Sprayed Fire Resistive Material (SFRM) Applied to Structural Members

E709-08	Standard Guide for Magnetic Particle Examination

E1155-96(R2008)	Determining FF Floor Flatness and FL Floor Levelness Numbers

F3125/F3125M-15	Standard Specification for High Strength Structural Bolts, Steel and Alloy Steel, Heat Treated, 120 ksi (830 MPa) and 150 ksi (1040 MPa) Minimum Tensile Strength, Inch and Metric Dimensions

E.	American Welding Society (AWS):

D1.D1.1M-10	Structural Welding Code-Steel

1.3 REQUIREMENTS:

A.	Accreditation Requirements: Construction materials testing laboratories must be accredited by a laboratory accreditation authority and will be required to submit a copy of the Certificate of Accreditation and Scope of Accreditation. The laboratory’s scope of accreditation must include the appropriate ASTM standards (i.e.; E329, C1077, D3666, D3740, A880, E543) listed in the technical sections of the specifications. Laboratories engaged in Hazardous Materials Testing shall meet the requirements of OSHA and EPA. The policy applies to the specific laboratory performing the actual testing, not just the “Corporate Office.”

B.	Inspection and Testing: Testing laboratory shall inspect materials and workmanship and perform tests described herein and additional tests requested by Resident Engineer. When it appears materials furnished, or work performed by Contractor fail to meet construction contract requirements, Testing Laboratory shall direct attention of Resident Engineer to such failure.

C.	Written Reports: Testing laboratory shall submit test reports to Resident Engineer, Contractor, unless other arrangements are agreed to in writing by the Resident Engineer. Submit reports of tests that fail to meet construction contract requirements on colored paper.

D.	Verbal Reports: Give verbal notification to Resident Engineer immediately of any irregularity.

PART 2 - PRODUCTS (Not Used)

PART 3 – EXECUTION (Not Used)

- - - E N D - - -