SECTION 04 05 13
MASONRY MORTARING

PART 1 - GENERAL

1.1 DESCRIPTION:

Section specifies mortar materials and mixes.

1.2 RELATED WORK:

A.	Mortar used in Section:

1.	Section 04 20 00, UNIT MASONRY.

B.	Mortar Color: Section 09 06 00, SCHEDULE FOR FINISHES.

1.3 TESTING LABORATORY-CONTRACTOR RETAINED

A.	Engage a commercial testing laboratory approved by Resident Engineer to perform tests specified below.

B.	Submit information regarding testing laboratory's facilities and qualifications of technical personnel to Resident Engineer.

1.4 TESTS (Not Used)

1.5 SUBMITTALS

A.	Submit in accordance with Section 01 33 23, SHOP DRAWINGS, PRODUCT DATA, AND SAMPLES.

B.	Certificates:

1.	Testing laboratory's facilities and qualifications of its technical personnel.

2.	Indicating that following items meet specifications:

a.	Portland cement.

b.	Masonry cement.

c.	Mortar cement.

d.	Hydrated lime.

e.	Fine aggregate (sand).

g.	Color admixture.

C.	Laboratory Test Reports:

1.	Mortar, each type.

2.	Admixtures.

D.	Manufacturer's Literature and Data:

1.	Cement, each kind.

2.	Hydrated lime.

3.	Admixtures.

4.	Liquid acrylic resin.

1.6 PRODUCT DELIVERY, STORAGE AND HANDLING

A.	Deliver masonry materials in original sealed containers marked with name of manufacturer and identification of contents.

B.	Store masonry materials under waterproof covers on planking clear of ground, and protect damage from handling, dirt, stain, water and wind.

1.7 APPLICABLE PUBLICATIONS

A.	Publications listed below form a part of specification to extent referenced. Publications are referenced in text by basic designation only.

B.	American Society for Testing and Materials (ASTM):

C40-04	Organic Impurities in Fine Aggregates for Concrete

C91-05	Masonry Cement

C109-08	Compressive Strength of Hydraulic Cement Mortars (Using 2-in. or 50-MM Cube Specimens)

C144-04	Aggregate for Masonry Mortar

C150-09	Portland Cement

C207-06	Hydrated Lime for Masonry Purposes

C270-10	Mortar for Unit Masonry

C307-03(R2008)	Tensile Strength of Chemical - Resistant Mortar, Grouts, and Monolithic Surfacing

C321-00(R2005)	Bond Strength of Chemical-Resistant Mortars

C348-08	Flexural Strength of Hydraulic Cement Mortars

C595-10	Blended Hydraulic Cement

C780-10	Preconstruction and Construction Evaluation of Mortars for Plain and Reinforced Unit Masonry

C979-10	Pigments for Integrally Colored Concrete

C1329-05	Mortar Cement

PART 2 - PRODUCTS

2.1 HYDRATED LIME

ASTM C207, Type S.

2.2 AGGREGATE FOR MASONRY MORTAR

A.	ASTM C144 and as follows:

1.	Light colored sand for mortar for laying face brick.

2.	White plastering sand meeting sieve analysis for mortar joints for pointing

B.	Test sand for color value in accordance with ASTM C40. Sand producing color darker than specified standard is unacceptable.

2.3 BLENDED HYDRAULIC CEMENT

ASTM C595, Type IS, IP.

2.4 MASONRY CEMENT

A.	ASTM C91. Type N, S, or M.

2.5 MORTAR CEMEMT

ASTM C1329, Type N, S or M.

2.6 PORTLAND CEMENT

A.	ASTM C150, Type I.

2.7 LIQUID ACRYLIC RESIN

A formulation of acrylic polymers and modifiers in liquid form designed for use as an additive for mortar to improve physical properties.

2.8 WATER

Potable, free of substances that are detrimental to mortar, masonry, and metal.

2.9 POINTING MORTAR

A.	For Cast Stone or Precast Concrete: Proportion by volume; One part white Portland cement, two parts white sand, and 1/5 part hydrated lime.

2.10 MASONRY MORTAR

A.	Conform to ASTM C270.

B.	Admixtures:

1.	Do not use mortar admixtures, and color admixtures // unless approved by Resident Engineer.

2.	Submit laboratory test report showing effect of proposed admixture on strength, water retention, and water repellency of mortar.

3.	Do not use antifreeze compounds.

C.	Colored Mortar:

1.	Maintain uniform mortar color for exposed work throughout.

2.	Match mortar color in approved sample or mock-up.

3.	Color of mortar for exposed work in alteration work to match color of existing mortar unless specified otherwise in section 09 06 00, SCHEDULE FOR FINISHES.

D.	Color Admixtures:

1.	Proportion as specified by manufacturer.

2.	For color, see Section 09 06 00, SCHEDULE FOR FINISHES.

brick.

2.11 COLOR ADMIXTURE

A.	Pigments: ASTM C979.

B.	Use mineral pigments only. Organic pigments are not acceptable.

C.	Pigments inert, stable to atmospheric conditions, nonfading, alkali resistant and water insoluble.

PART 3 - EXECUTION

3.1 MIXING

A.	Mix in a mechanically operated mortar mixer.

1.	Mix mortar for at least three minutes but not more than five minutes.

B.	Measure ingredients by volume. Measure by the use of a container of known capacity.

C.	Mix water with dry ingredients in sufficient amount to provide a workable mixture which will adhere to vertical surfaces of masonry units.

D.	Mortar that has stiffened because of loss of water through evaporations:

1.	Re-tempered by adding water to restore to proper consistency and workability.

2.	Discard mortar that has reached its initial set or has not been used within two hours.

E.	Pointing Mortar:

1.	Mix dry ingredients with enough water to produce a damp mixture of workable consistency which will retain its shape when formed into a ball.

2.	Allow mortar to stand in dampened condition for one to 1-1/2 hours.

3.	Add water to bring mortar to a workable consistency prior to application.

3.2 MORTAR USE LOCATION

A.	Use Type M mortar for waterproof parging below grade.

B.	Use Type S mortar for masonry below grade.

C.	For brick veneer over frame back up walls, use Type N portland cement-lime mortar or Type S masonry cement or mortar cement mortar.

D.	Use Type N mortar for other masonry work, except as otherwise specified.

- - - E N D - - -