# SECTION 04 05 16
MASONRY GROUTING

GENERAL

## SUMMARY

Section Includes: Grout for filling hollow concrete masonry cores.

## RELATED WORK

Section 03 45 00, PRECAST ARCHITECTURAL CONCRETE: Grout

Section 04 20 00, UNIT MASONRY: Grout

Section 04 72 00, CAST STONE MASONRY: Grout

Section 09 06 00, SCHEDULE FOR FINISHES: Grout Color

Section 09 30 13, CERAMIC/PORCELAIN TILING: Ready-Mixed Grout.

Section 09 91 00, PAINTING

## APPLICABLE PUBLICATIONS

Comply with references to extent specified in this section

American National Standards Institute (ANSI):

A118.6-19 - 	Standard Cement Grouts for Tile Installation.

ASTM International (ASTM):

C40/C40M-20 - 	Organic Impurities in Fine Aggregates for Concrete.

C150/C150M-20 - 	Portland Cement.

C207-18 - 	Hydrated Lime for Masonry Purposes.

C404-18 - 	Aggregates for Masonry Grout.

C476-20 - 	Grout for Masonry.

C595/C595M-20 - 	Blended Hydraulic Cement.

C979/C979M-16 - 	Pigments for Integrally Colored Concrete.

C1019-19 - 	Sampling and Testing Grout.

## SUBMITTALS

Submittal Procedures: Section 01 33 23, SHOP DRAWINGS, PRODUCT DATA, AND SAMPLES. All items indicated below are required submittals requiring Contracting Officer’s Representative (COR) review and approval.

Manufacturer's Literature and Data:

Description of each product.

Sustainable Construction Submittals:

Recycled Content: Identify pre-consumer recycled content percentage by weight.

Test Reports: Certify each product complies with specifications.

Grout, each type.

Cement.

Aggregate.

Certificates: Certify each product complies with specifications.

Blended hydraulic cement.

Portland cement.

Grout.

Hydrated lime.

Aggregate.

Color admixture.

## QUALITY ASSURANCE

Preconstruction Testing:

Engage independent testing laboratory to perform tests and submit reports.

Deliver samples to laboratory in number and quantity required for testing.

Grout:

Test compressive strength according to ASTM C1019 standard.

Cement:

Test for water soluble alkali (nonstaining) when nonstaining cement is specified.

Nonstaining cement containing more than 0.03 percent water soluble alkali.

Aggregate:

Test for deleterious substances, organic impurities, soundness and grading.

## DELIVERY

Deliver products in manufacturer's original sealed packaging.

Mark packaging, legibly. Indicate manufacturer's name or brand, type, production run number, and manufacture date.

STORAGE AND HANDLING

Store masonry materials under waterproof covers on planking clear of ground, and protect damage from handling, dirt, stain, water and wind.

Protect products from damage during handling and construction operations.

## WARRANTY

Construction Warranty: FAR clause 52.246-21, "Warranty of Construction."

PRODUCTS

## MATERIALS

Grout Components:

Hydrated Lime: ASTM C207, Type S.

Aggregate For Masonry Grout: ASTM C404, Size 8.

Blended Hydraulic Cement: ASTM C595, Type IS, IP.

Portland Cement: ASTM C150, Type I.

Liquid Acrylic Resin:

A formulation of acrylic polymers and modifiers in liquid form designed for use as an additive for mortar to improve physical properties.

Water: Potable, free of substances that are detrimental to grout, masonry, and metal.

## PRODUCTS - GENERAL

Provide each product from one manufacturer.

Sustainable Construction Requirements:

Select products with recycled content to achieve overall Project recycled content requirement.

Combined Fly Ash and Pozzolan: 25 percent total recycled content, minimum.

Ground Granulated Blast-Furnace Slag: 50 percent total recycled content, minimum.

## MIXES

Grout: ASTM C476; fine grout and coarse grout.

Color Admixture:

Pigments: ASTM C979, inert, stable to atmospheric conditions, nonfading, alkali resistant, and water insoluble.

Use mineral pigments only. Organic pigments are not acceptable.

Ready-Mixed Grout: ANSI A118.8.

EXECUTION

## PREPARATION

Examine and verify substrate suitability for product installation.

Protect existing construction and completed work from damage.

Clean mortar from masonry cells protruding more than 13 mm (1/2 inch) to permit grout flow.

Remove debris from grout spaces.

Verify reinforcement is correctly placed before placing grout.

## MIXING

Mix grout in mechanically operated mixer.

Mix grout for five minutes, minimum.

Measure ingredients by volume using container of known capacity.

Mix water with grout dry ingredients.

Slump Range: 200 to 275 mm (8 to 11 inches).

## GROUTING

Install grout according to Section 04 20 00, UNIT MASONRY.

Use fine grout for filling wall cavities and hollow concrete masonry units where smallest cell dimension is 50 mm (2 inches) or less.

Use either fine grout or coarse grout for filling wall cavities and hollow concrete masonry units where smallest cell dimension is greater than 50 mm (2 inches).

Use grout for filling bond beam or lintel units.

- - E N D - -