SECTION 07 22 00

ROOF AND DECK INSULATION

GENERAL

SUMMARY

Section Includes:

Roof and deck insulation, substrate board, vapor retarder, and cover board on existing concrete deck substrates ready to receive roofing or waterproofing membrane.

Repairs and alteration work to existing roof insulation.

RELATED REQUIREMENTS

Non-Flooring Adhesives and Sealants VOC Limits: Section 01 81 13, SUSTAINABLE CONSTRUCTION REQUIREMENTS.

Wood Cants, Blocking, and Edge Strips: Section 06 10 00, ROUGH CARPENTRY.

APPLICABLE PUBLICATIONS

Comply with references to extent specified in this section.

American Society of Heating, Refrigeration and Air Conditioning (ASHRAE):

Standard 90.1-13 - Energy Standard for Buildings Except Low-Rise Residential Buildings.

ASTM International (ASTM):

C208-12 - Cellulosic Fiber Insulating Board.

C552-15 - Cellular Glass Thermal Insulation.

C726-05 - Mineral Fiber Roof Insulation Board.

C728-15 - Perlite Thermal Insulation Board.

C1177/C1177M-13 - Glass Mat Gypsum Substrate for Use as Sheathing.

C1278/C1278M-07a(2015) - Fiber-Reinforced Gypsum Panel.

C1289-15 - Faced Rigid Cellular Polyisocyanurate Thermal Insulation Board.

C1396/C1396M-14a - Gypsum Board.

D41/D41M-11 - Asphalt Primer Used in Roofing, Damp-proofing, and Waterproofing.

D312-06 - Asphalt Used in Roofing.

D1970/D1970M-15 - Self-Adhering Polymer Modified Bituminous Sheet Materials Used as Steep Roofing Underlayment for Ice Dam Protection.

D2178/D2178M-15 - Asphalt Glass Felt Used in Roofing and Waterproofing.

D2822/D2822M-11 - Asphalt Roof Cement, Asbestos Containing.

D4586/D4586M-07(2012)e1 - Asphalt Roof Cement, Asbestos-Free.

E84-15a - Surface Burning Characteristics of Building Materials.

F1667-15 - Driven Fasteners: Nails, Spikes, and Staples.

National Roofing Contractors Association (NRCA):

Manual-15 - The NRCA Roofing Manual: Membrane Roof Systems.

U.S. Department of Agriculture (USDA):

USDA Bio-Preferred Program Catalog.

UL LLC (UL):

Listed - Online Certifications Directory.

U.S. Department of Commerce National Institute of Standards and Technology (NIST):

DOC PS 1-09 - Structural Plywood.

DOC PS 2-04 - Performance Standard for Wood-Based Structural-Use Panels.

SUBMITTALS

Submittal Procedures: Section 01 33 23, SHOP DRAWINGS, PRODUCT DATA, AND SAMPLES.

Submittal Drawings:

Show size, configuration, and installation details.

Nailers, cants, and terminations.

Layout of insulation showing slopes, tapers, penetrations, and edge conditions.

Manufacturer's Literature and Data:

Description of each product.

Samples:

Roof insulation, each type.

Fasteners, each type.

Sustainable Construction Submittals:

Recycled Content: Identify post-consumer and pre-consumer recycled content percentage by weight.

Biobased Content:

Show type and quantity for each product.

Low Pollutant-Emitting Materials:

Show volatile organic compound types and quantities.

Certify each composite wood and agrifiber product contain no added urea formaldehyde.

Qualifications: Substantiate qualifications meet specifications.

Installer.

QUALITY ASSURANCE

Installer Qualifications: Same installer as Division 07 roofing section installer.

DELIVERY

Comply with recommendations of NRCA Manual.

Deliver products in manufacturer's original sealed packaging.

Mark packaging, legibly. Indicate manufacturer's name or brand, type, and manufacture date.

Before installation, return or dispose of products within distorted, damaged, or opened packaging.

STORAGE AND HANDLING

Comply with recommendations of NRCA Manual.

Store products indoors in dry, weathertight facility.

Protect products from damage during handling and construction operations.

FIELD CONDITIONS

Environment:

Install products when existing and forecasted weather permit installation according to manufacturer's instructions.

WARRANTY

Construction Warranty: FAR clause 52.246-21, "Warranty of Construction."

Manufacturer's Warranty: Warrant substrate board, vapor retarder, insulation, and cover board against material and manufacturing defects as part of Division 07 roofing system warranty.

PRODUCTS

SYSTEM PERFORMANCE

Insulation Thermal Performance:

Overall Average R-Value: RSI-57 (R-33), minimum.

Any Location R-Value: RSI-17 (R-10), minimum.

Fire and Wind Uplift Resistance: Provide roof insulation complying with requirements specified in Division 07 roofing section.

Insulation on Concrete Deck surface: UL labeled indicating compliance with one of the following:

UL Listed.

Insulation Surface Burning Characteristics: When tested according to ASTM E84.

Flame Spread Rating: 75 maximum.

Smoke Developed Rating: 150 maximum.

PRODUCTS - GENERAL

Provide each product from one manufacturer.

Sustainable Construction Requirements:

Insulation Recycled Content:

Mineral Fiber: 75 percent total recycled content, minimum.

Fiberglass: 20 percent total recycled content, minimum.

Cellulose: 75 percent post-consumer recycled content, minimum.

Perlite Composite Board: 23 percent post-consumer recycled content, minimum.

Rigid Foam: 9 percent total recycled content, minimum.

Glass Fiber Reinforced Rigid Foam: 6 percent total recycled content, minimum.

Low Pollutant-Emitting Materials: Comply with VOC limits specified in Section 01 81 13, SUSTAINABLE CONSTRUCTION REQUIREMENTS for the following products:

Non-flooring adhesives and sealants.

Composite wood and agrifiber.

Bio-Based Materials: Where applicable, provide products designated by USDA and meeting or exceeding USDA recommendations for bio-based content, and products meeting Rapidly Renewable Materials and certified sustainable wood content definitions; refer to www.biopreferred.gov.

ADHESIVES

Primer: ASTM D41/D41M.

Bead-Applied Urethane Insulation Adhesive: Insulation manufacturer's recommended bead-applied, low-rise, one- or multicomponent urethane adhesive formulated to adhere roof insulation to substrate or to another insulation layer.

Full-Spread Applied Urethane Insulation Adhesive: Insulation manufacturer's recommended spray-applied, low-rise, two-component urethane adhesive formulated to adhere roof insulation to substrate or to another insulation layer.

Roof Cement: Asbestos free, ASTM D2822/D2822M, Type I or Type II; or, ASTM D4586/D4586M, Type I or Type II.

ROOF AND DECK INSULATION

Roof and Deck Insulation, General: Preformed roof insulation boards approved by roofing manufacturer.

Polyisocyanurate Board Insulation: ASTM C1289, Type II, Class 1, Grade 2, faced with glass fiber reinforced cellulosic felt facers on both major surfaces of the core foam.

Cellular Glass Board Insulation: ASTM C552, Type IV, kraft-paper sheet faced.

Cellulosic Fiber Board Insulation: ASTM C208, Type II, Grade 1 for built-up asphalt or modified bitumen roofing, and Grade 2 for single-ply roofing.

Tapered Roof Insulation System:

Fabricate of mineral fiberboard, polyisocyanurate, perlite board, or cellular glass. Use only one insulation material for tapered sections. Use only factory-tapered insulation.

Cut to provide high and low points with crickets and slopes as shown.

Minimum thickness of tapered sections; 38 mm (1-1/2 inch).

Minimum slope 1/48 (1/4 inch per 12 inches).

Composite Nail Base Insulated Roof Sheathing:

Oriented-Strand-Board-Surfaced, Polyisocyanurate-Foam Sheathing: Polyisocyanurate thermal insulation ASTM C1289, Type V, insulation thickness as shown, with oriented strand board laminated to top surface.

Oriented Strand Board: NIST DOC PS 1, Exposure 1, 16 mm (5/8 inch) thick.

Bottom surface faced with felt facers.

INSULATION ACCESSORIES

Cants and Tapered Edge Strips:

Insulation Cant Strips: ASTM C208, Type II, Grade 1, cellulosic-fiber insulation board.

Tapered Edge Strips: 1/12 (1 inch per 12 inches), from 0 mm (0 inches), 300 mm to 450 mm (12 inches to 18 inches) wide.

Cellulosic Fiberboard: ASTM C208.

Mineral Fiberboard: ASTM C726.

Perlite Board: ASTM C728.

Tapered Insulation for Roof Water Control, Tapered Insulation Drainage Cricket Boards, 1/12 (1 inch per 12 inches), from 0 mm

Vapor Retarder:

Glass-Fiber Felts: ASTM D2178/D2178M, Type IV, asphalt impregnated.

Self-Adhering Sheet Vapor Retarder: ASTM D1970/D1970M, minimum 1.0 mm (40 mils) thick membrane of HDPE film fully coated with asphalt adhesive, or 0.76 to 1.0 mm (30 to 40 mils) thick membrane of butyl rubber based adhesive backed by a layer of high density cross-laminated polyethylene; maximum permeance rating of 6 ng/Pa/s/sq. m (0.1 perms).

Substrate Board:

Glass-Mat, Water-Resistant Gypsum Roof Board: ASTM C1177/C1177M, Type X, 16 mm (5/8 inch) thick, factory primed.

Cellulosic-Fiber-Reinforced, Water-Resistant Gypsum Roof Board: ASTM C1278/C1278M, 16 mm (5/8 inch) thick.

Cover Board:

Glass-Mat, Water-Resistant Gypsum Roof Board: ASTM C1177/C1177M, 16 mm (5/8 inch) thick, factory primed.

Cellulosic-Fiber-Reinforced, Water-Resistant Gypsum Roof Board: ASTM C1278/C1278M, 16 mm (5/8 inch) thick.

Cellulosic-Fiber Insulation Board: ASTM C208, Type II, Grade 2, 13 mm (1/2 inch) thick.

Oriented Strand Board: DOC PS 2, Exposure 1, 11 mm (7/16 inch) thick.

ACCESSORIES

Fasteners: Corrosion-resistant carbon steel fasteners and galvalume-coated steel or plastic round plates for fastening substrate board and insulation to roof deck.

Nails: ASTM F1667; type to suit application.

EXECUTION

EXAMINATION

Comply with requirements of Division 07 roofing section.

PREPARATION

Examine and verify substrate suitability for product installation.

Protect existing construction and completed work from damage.

INSTALLATION - GENERAL

Install products according to manufacturer's instructions.

When manufacturer's instructions deviate from specifications, submit proposed resolution for Contracting Officer's Representative consideration.

Comply with requirements of UL for insulated steel roof deck.

Attach substrate board and other products to meet requirements of Division 07 roofing section.

VAPOR RETARDER INSTALLATION

Vapor Retarder Installation, General:

Install continuous vapor retarder on roof decks where indicated.

At vertical surfaces, turn up vapor retarder to top of insulation or base flashing.

Seal penetrations through vapor retarder with roof cement to prevent moisture entry from below.  Cements must be compatible with roofing system

Cast in Place Concrete Decks, Except Insulating Concrete:

Prime deck as specified.

Apply a single ply of waterproof roofing membrane compatible with the roofing system adhered to the concrete roof deck with the roofing system adhesive.

Precast Concrete Unit Decks Without Concrete Topping:

Prime deck as specified.

Apply a single ply of waterproof roofing membrane compatible with the roofing system adhered to the concrete roof deck with the roofing system adhesive.

Insulation Installation, General:

Base Sheet: Where required by roofing system, install one lapped base sheet specified in Division 07 roofing section by mechanically fastening to roofing substrate before installation of insulation.

Cant Strips: Install preformed insulation cant strips at junctures of roofing system with vertical construction.

Use same insulation as existing for roof repair and alterations unless specified otherwise.

Insulation Thickness:

Thickness of roof insulation shown on drawings is nominal. Provide thickness required to comply with specified thermal performance.

Insulation on Metal Decks: Provide insulation in minimum thickness recommended by insulation manufacturer to span deck flutes. Support edges of insulation on metal deck ribs.

When actual insulation thickness differs from drawings, coordinate alignment and location of roof drains, flashing, gravel stops, fascias and similar items.

Where tapered insulation is used, maintain insulation thickness at high points and roof edges shown on drawings.

Low Point Thickness: Minimum 38 mm (1-1/2 inches).

Use minimum two layers of insulation when required thickness is 68 mm (2.7 inch) or greater.

Lay insulating units with close joints, in regular courses and with end joints staggered.

Stagger joints between layers minimum 150 mm (6 inches).

Lay units with long dimension perpendicular to the rolled (longitudinal) direction of the roofing felt.

Cover all insulation installed on the same day; comply with temporary protection requirements of Division 07 roofing section.

Installation Method:

Adhered Insulation:

Prime substrate as required.

Set each layer of insulation firmly in a roller applied adhesive.

Set each layer of insulation firmly in ribbons of bead-applied insulation adhesive.

Set each layer of insulation firmly in uniform application of full-spread insulation adhesive.

Adhered Insulation:

Fasten first layer of insulation according to " Adhered Insulation " requirements.

Fasten each subsequent layer of insulation according to "Adhered Insulation" requirements.

COVER BOARD INSTALLATION

Install cover boards over insulation with long joints in continuous straight lines with staggered end joints.

Offset cover board joints from insulation joints 150 mm (6 inches), minimum.

Secure cover boards according to "Adhered Insulation" requirements.

- - E N D - -